铝、钢、铜及常用合金材料性能总表（**一键复制直接粘贴Excel**、英文表头、含加工难度）

使用说明：全选下方表格 → 复制 → 直接粘贴进 Excel，自动分列、无错乱格式

| Material | Density(g/cm³) | Thermal Conductivity(W/m·K) | Conductivity Type | Specific Heat(J/kg·K) | Melting Point(℃) | Thermal Expansion(ppm/℃) | Elastic Modulus(GPa) | Poissons Ratio | Shear Modulus(GPa) | Tensile Strength(MPa) | Compressive Strength(MPa) | Yield Strength(MPa) | Processing Difficulty | Processing Characteristics |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Pure Aluminum | 2.70 | 205 | Metallic Conductor | 900 | 660 | 23.0 | 69 | 0.33 | 26 | 110 | Similar to yield | 55 | Very Easy | Soft,good ductility,easy bending&stamping |
| Aluminum Alloy 6061 | 2.70 | 167 | Metallic Conductor | 897 | 652 | 23.5 | 69 | 0.33 | 26 | 310 | Similar to yield | 240 | Easy | Balanced performance,easy cutting&welding |
| Aluminum Alloy 7075 | 2.80 | 130 | Metallic Conductor | 960 | 635 | 23.2 | 71 | 0.33 | 27 | 572 | Similar to yield | 503 | Medium | High strength,hard cutting,difficult welding |
| Mild Carbon Steel | 7.85 | 48 | Metallic Conductor | 450 | 1450 | 12.0 | 206 | 0.30 | 79 | 440 | ≥450 | 275 | Easy | Good weldability,low cost,easy machining |
| 45# Carbon Steel | 7.85 | 45 | Metallic Conductor | 460 | 1445 | 11.5 | 208 | 0.29 | 80 | 600 | ≥620 | 355 | Medium | Need preheating before welding,hardened after quenching |
| 304 Stainless Steel | 7.93 | 17 | Metallic Conductor | 470 | 1430 | 17.3 | 193 | 0.29 | 75 | 505 | ≥510 | 205 | Medium | Poor thermal conductivity,easy tool sticking |
| Pure Copper | 8.96 | 401 | Metallic Conductor | 385 | 1083 | 16.5 | 110 | 0.34 | 45 | 210 | Similar to yield | 70 | Medium | Excellent ductility,easy deformation during welding |
| Brass | 8.50 | 125 | Metallic Conductor | 377 | 920 | 19.0 | 105 | 0.34 | 40 | 380 | ≥400 | 150 | Easy | Best cutting property among copper alloys |
| Bronze | 8.80 | 62 | Metallic Conductor | 360 | 950 | 18.0 | 115 | 0.35 | 43 | 450 | ≥480 | 200 | Medium | High hardness,wear resistance,strict cutting requirement |

## 附加中文简表（方便对照学习，可选择性复制）

| 材料 | 密度 | 导热系数 | 导电类型 | 比热容 | 熔点 | 热膨胀系数 | 弹性模量 | 泊松比 | 剪切模量 | 抗拉强度 | 抗压强度 | 屈服强度 | 加工难度 | 加工特点 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 纯铝 | 2.70 | 205 | 金属导体 | 900 | 660 | 23.0 | 69 | 0.33 | 26 | 110 | 近似屈服强度 | 55 | 极易 | 质软、折弯冲压极好 |
| 6061 铝合金 | 2.70 | 167 | 金属导体 | 897 | 652 | 23.5 | 69 | 0.33 | 26 | 310 | 近似屈服强度 | 240 | 容易 | 综合性能均衡、切削焊接简单 |
| 7075 航空铝 | 2.80 | 130 | 金属导体 | 960 | 635 | 23.2 | 71 | 0.33 | 27 | 572 | 近似屈服强度 | 503 | 中等 | 硬度高、切削难、不易焊 |
| 低碳钢 | 7.85 | 48 | 金属导体 | 450 | 1450 | 12.0 | 206 | 0.30 | 79 | 440 | ≥450 | 275 | 容易 | 焊接极好、成本最低 |
| 45 号钢 | 7.85 | 45 | 金属导体 | 460 | 1445 | 11.5 | 208 | 0.29 | 80 | 600 | ≥620 | 355 | 中等 | 调质变硬、焊接需要预热 |
| 304 不锈钢 | 7.93 | 17 | 金属导体 | 470 | 1430 | 17.3 | 193 | 0.29 | 75 | 505 | ≥510 | 205 | 中等 | 导热差、切削粘刀 |
| 纯铜 | 8.96 | 401 | 金属导体 | 385 | 1083 | 16.5 | 110 | 0.34 | 45 | 210 | 近似屈服强度 | 70 | 中等 | 延展性顶级、焊接易变形 |
| 黄铜 | 8.50 | 125 | 金属导体 | 377 | 920 | 19.0 | 105 | 0.34 | 40 | 380 | ≥400 | 150 | 容易 | 铜合金中最好切削 |
| 青铜 | 8.80 | 62 | 金属导体 | 360 | 950 | 18.0 | 115 | 0.35 | 43 | 450 | ≥480 | 200 | 中等 | 耐磨硬度高、加工要求严格 |

## 三大材料加工难度总结（极简总结）

Aluminum 铝合金：加工最简单，质地软、阻力小

Copper 铜合金：易塑形、难切削，纯铜最粘刀

Steel 钢材：硬度越高加工越难，不锈钢最难加工

|（注：文档部分内容可能由 AI 生成）